| Colour | Product Code | Pack Size | Box Qty |
| --- | --- | --- | --- |
| - | ZERO5 | 5Ltr | 4 |
|  | ZEROM25 | 25Ltr | 1 |

Product Description

EVERBUILD ZEROMIX CFF is air entraining chloride free liquid admixture for mortar and concrete which also acts as an accelerator for work in sub - zero temperatures. Improves workability and freeze/thaw resistance in brick laying mortars and eliminates 	the need for a separate frostproofer. Conforms to EN934-3 (2009)

Benefits

- Increased frost resistance during setting.

- Non - corrosive to imbedded metal (chloride ion free)

- Eases tamping down and alignment

- Improves workability/trowelability even in cold weather.

- Provides resistance to freeze/thaw cycling down to -8oC in both wet and dry mortar.

- Chloride free (chloride ion content < 0.1%).

- Reduces bleeding/segregation.

- Replaces lime in mix, hence reduces possibility of lime bloom and efflorescence.

- Reduces shrinkage (cracking and crazing reduced).

- Faster finishing times even in cold weather.

Areas For Use

As an air entraining water reducing admixture and accelerator/frostproofer for brick and block laying mortar, render (internal and external) and concrete. Accelerates setting time during cold periods. Suitable for:

- Load bearing brickwork

- Block laying

- External/Internal rendering

- Pointing/repointing brickwork.

- Floor screeds

Limitations

- Concrete must be covered after placing until the minimum strength is  obtained or until the temperature rises above freezing.

- Do not use weak mixes during cold weather.

- Do not overdose.

Surface Preparation

All materials used must be free from ice and the temperature of the mix prior to placing not be less than 4oC. Concrete must be covered after placing until the minimum strength is obtained or until the temperature rises above freezing. Do not use weak mixes during cold weather.

Application

Work should be carried out in accordance with the methods outlined in the Code of Practice BS5628 Part 3 for protection and use of mortars at low temperatures and  DOE Advisory Leaflet No. 8. In all cases, add to mix at an addition rate of 2.5 to 5 litres per 50kg cement depending on the degree of plasticising/acceleration required. Note: remember to reduce required quantity of water accordingly. Alternatively, add to mixing drum at same time as water.

The following are examples of modified mix designs.

1: 0.25 :3  cement : lime : sand.   		.

use 1 : 3  cement : sand : + ZEROMIX CFF

1:1:6 cement : lime : sand

use 1 : 6  cement : sand + ZEROMIX CFF

BRICKLAYING/POINTING		Use a mix design appropriate to brick strength (1 : 3  to 1 : 6).

INTERNAL RENDERS		1 : 6  + ZEROMIX CFF

EXTERNAL RENDERS		1 : 3 + ZEROMIX CFF

Specific Data

| Appearance | Clear/Amber Liquid |
| --- | --- |
| Specific Gravity @ 20°C | 1.2 |
| Freezing Point | - |
| pH | 9 |
| Chloride Ion Content | < 0.1% w/w (nil) |
| Dosage | Ambient temperatures down to -4°C: 2.5Litres per 50Kg cement Ambient temperatures below -4°C: 5Litres per 50Kg cement |
| Typical Reduction In Setting Times | 20-30% (@ 2.5Ltr/50Kg cement) |

Health & Safety

Consult MSDS for full list of hazards.

Storage

Store at moderate temperatures. Will reconstitute after freezing.

Shelf Life

24 months from date of manufacture when stored according to manufacturer’s instructions.

The technical data contained herein is based on our present knowledge and experience and we cannot be held liable for any errors, inaccuracies, omissions or editorial failings that result from technological changes or research between the date of issue of this document and the date the product is acquired. Before using the product, the user should carry out any necessary tests in order to ensure that the product is suitable for the intended application. Moreover, all users should contact the seller or the manufacturer of the product for additional technical information concerning its use if they think that the information in their possession needs to be clarified in any way, whether for normal use or a specific application of our product. Our guarantee applies within the context of the statutory regulations and provisions in force, current professional standards and in accordance with the stipulations set out in our general sales conditions. The information detailed in the present technical data sheet is given by way of indication and is not exhaustive. The same applies to any information provided verbally by telephone to any

prospective or existing customer.

# Text boxes

EVERBUILD 207 ZEROMIX CFF

Site 41, Cross Green Industrial estate,

Knowsthorpe Way, Leeds

LS9 0SW

11

0086-CPD-565048

EN934-3 (2009)

Air entraining/plasticizing admixture for masonry mortar

EN934-3, T2.

Chloride content: <0.1% w/w

Alkali content : 0.1% by mass

Corrosion behaviour2 : NPD