| Colour | Product Code | Pack Size | Box Qty |
| --- | --- | --- | --- |
| Black | 90205 | 5Ltr | 4 |
|  | 90205 | 25Ltr | 1 |

Product Description

BLACK JACK BITUMEN PRIMER is a thin black primer used to give a key prior to applying bitumen paints and roof coatings. Also suitable as a primer prior to applying BLACK JACK FLASHING TAPE.

Benefits

- Fast drying.

- Suitable for use with all bituminous surface coatings

Areas For Use

Mainly used for priming:

- Concrete roofs and floors, cementicious screeds and renders,

- Bitumen felt, asphalt and mastic

- Weathered corrugated iron and steel.

- Wood.

Limitations

- Do not use in areas where subsequent solvent contact is likely.

- Avoid inhalation of vapours in confined spaces.

- Allow sufficient drying time before overcoating.

Surface Preparation

As with all surface coatings, preparation of the surface is of great importance and will influence the degree of adhesion obtained and the life of the coating, All surfaces must be sound, stable and thoroughly clean and dry.  Metal surfaces should be wire brushed to remove rust.  Where long term protection is required an initial treatment of a rust inhibitive product such as red lead or zinc phosphate should be used. Loose or blistered paint should be removed as should tar based paint systems. New galvanised surfaces should be roughened with a wire brush or treated with a proprietary etch primer.

Application

BLACK JACK BITUMEN AND FLASHING PRIMER is ready for use and should not be thinned. Apply by brush or spray.

The primer should be well scrubbed in by brush. ensuring  a thin even coverage. Avoid ponding/pooling when applying by spray.

With fibre cement or rag felt, apply generously to saturate the surface.

CLEANING TOOLS

Tools may be cleaned by using white spirit.  Spillage’s should be wiped off surfaces before the primer has set.

Specific Data

| Type Of Solvent | White spirits |
| --- | --- |
| Flashpoint | 40°C |
| Specific Gravity @ 20°C | 0.9 |
| Coverage | 4 -6m² per litre depending on porosity of subsrate 11m² per litre on non porous surfaces |
| Drying Time | 3 -6 hours depending on drying conditions |
| Service Temps | -20 to +50°C |
| Application Temps | 5 to 50°C. Surfaces must be free from ice and water |
| Specification | - |
| Film Thickness Per Coat @ 11m²/Ltr | Wet – 0.1mm Dry – 0.05mm |
| Chemical And Water Resistance | Resistant to: most salt solutions, dilute acids and alkalis, water and alcohol. Not resistant to: oils, solvents and some detergent solutions. |

Health & Safety

Consult MSDS for full list of hazards.

Storage

BLACK JACK BITUMEN AND FLASHING PRIMER contains a flammable solvent, and all normal precautions against fire must be taken during both storage and use.  Store in original container in cool dry conditions.  Keep away from sources of ignition.

Shelf Life

Storage life 24 months in tightly sealed, undamaged containers.

The technical data contained herein is based on our present knowledge and experience and we cannot be held liable for any errors, inaccuracies, omissions or editorial failings that result from technological changes or research between the date of issue of this document and the date the product is acquired. Before using the product, the user should carry out any necessary tests in order to ensure that the product is suitable for the intended application. Moreover, all users should contact the seller or the manufacturer of the product for additional technical information concerning its use if they think that the information in their possession needs to be clarified in any way, whether for normal use or a specific application of our product. Our guarantee applies within the context of the statutory regulations and provisions in force, current professional standards and in accordance with the stipulations set out in our general sales conditions. The information detailed in the present technical data sheet is given by way of indication and is not exhaustive. The same applies to any information provided verbally by telephone to any prospective or existing customer.

# Text boxes

902 BITUMEN & FLASHING PRIMER