| Colour | Product Code | Pack Size | Box Qty |
| --- | --- | --- | --- |
| Grey | EPOX1054 | 4KG | 1 |
|  | EPOX10514 | 14KG | 1 |

Product Description

EVERBUILD EPOXYSET 105 is a three-part general purpose repair mortar based on epoxy resin technology. EPOXY SET 105 is formulated to withstand chemicals, impact and abrasion and can be used to repair concrete, screeds, stone, brick and steel in even the most demanding domestic and industrial situations. EPOXYSET 105 is the ideal product for repairing floors, steps, pipes, kerbs and sills. EPOXYSET 105 is also the ideal choice for repairing cracks in masonry and concrete.

Benefits

- Excellent chemical resistance

- Excellent impact and wear resistance.

- Can be laid in thin sections.

- Greater physical strength than conventional cementicious systems.

Areas For Use

- Heavy traffic areas

- Steps

- Walkways/Ramps

- Industrial floors

Limitations

- Always mix as directed using all three components.

- Do not use where application would trap moisture within the substrate or in situations where hydrostatic pressure could break the bond

- As the manufacturer cannot know all the uses its products may be put to, it is the users responsibility to determine suitability for use. If in doubt, contact technical services department for advice.

Surface Preparation

Ensure surfaces are free from flaking material, dust, rust and grease. Saw/chisel edges to a defined area to a depth of 3mm. When applying to steel, shot blast, grind, or emery to a bright finish and remove residues.

Application

Before use, wear impervious gloves provided. Thoroughly mix components A and B with mixing stick and pour into suitable mixing vessel. Add the aggregate to this solution and mix thoroughly with a slow speed drill and paddle. Trowel to desired finish with a clean steel trowel. Wipe the trowel intermittently with finishing solvent to reduce drag.

Coverage: 	4kg of mixed product will cover approximately 1m2 at 3mm depth.

Pot Life:	The pot life of this product is 20-25 minutes at 20oC. Low temperatures will retard the cure. Do not apply below 4oC.

Cure Time:	Initial: 24 hours. Final: 7 days. Do not traffic for 24 hours. If a faster cure is required, use EVERBUILD EPOXY SET 106 (one hour cure)

Storage: 	Store in cool, dry conditions away from direct sunlight. Keep in original containers.

Cleaning:	Clean tools etc with finishing solvent.

Specific Data

| Density (mixed) | 2.03g/cm3 |
| --- | --- |
| Application /curing temps | +4 to +40°C |
| Service Temperature | -20 to +50°C |
| Compressive strength (BS6319 part 2) | 50N/mm2 @24 hours (20°C) |
| Tensile strength | 15N/mm2 @ 7 days (20°C) |
| Abrasion resistance | High |
| Adhesive strength to concrete | Greater than the internal tensile strength of concrete |

Health & Safety

Consult MSDS for full list of hazards.

Storage

Store in cool dry conditions between + 5°C and 25°C.

Shelf Life

24 months from date of manufacture.

The technical data contained herein is based on our present knowledge and experience and we cannot be held liable for any errors, inaccuracies, omissions or editorial failings that result from technological changes or research between the date of issue of this document and the date the product is acquired. Before using the product, the user should carry out any necessary tests in order to ensure that the product is suitable for the intended application. Moreover, all users should contact the seller or the manufacturer of the product for additional technical information concerning its use if they think that the information in their possession needs to be clarified in any way, whether for normal use or a specific application of our product. Our guarantee applies within the context of the statutory regulations and provisions in force, current professional standards and in accordance with the stipulations set out in our general sales conditions. The information detailed in the present technical data sheet is given by way of indication and is not exhaustive. The same applies to any information provided verbally by telephone to any prospective or existing customer.

# Text boxes

EVERBUILD EPOXYSET 105